PerkinElmer Spectrum Version 10.4.3
Monday, May 04, 2015 5:00 PM

Report Details
Report Location	C:\Users\Didattica\Desktop\chim_fis_2\2015\a3a4\polystirene_ir 39.rtf	
Report Creator	user	
Report Date	Monday, May 04, 2015 5:00 PM	

Spectrum
	
Name	Description	
 ___  ir 39	Sample 039 By ir Date Monday, May 04 2015	

Summary
Sample Name	Description	Quality	
ir 39	Sample 039 By ir Date Monday, May 04 2015	The Quality Checks give rise to multiple warnings for the sample.	

Peak Table Spectrum

Peak Table
Peak No.	X (cm-1)	Y (A)	Peak No.	X (cm-1)	Y (A)	Peak No.	X (cm-1)	Y (A)	
1	4658.9	0.1006	2	4336.17	0.0972	3	4210.35	0.1075	
4	4036.53	0.1631	5	3895.7	0.0963	6	3832.34	0.0973	
7	3768.82	0.0957	8	3646.75	0.1146	9	3582.86	0.0947	
10	3519.04	0.093	11	3455.6	0.0972	12	3392.95	0.0941	
13	3331.17	0.0937	14	3269.55	0.0964	15	3206.37	0.1043	
16	3103.16	0.3968	17	3082.62	1.0772	18	3060.38	1.4977	
19	3025.81	2.8839	20	3001.61	0.6431	21	2924.45	3.074	
22	2850.03	1.028	23	2747.24	0.1241	24	2687.51	0.1309	
25	2630.49	0.1368	26	2563.21	0.1226	27	2502.34	0.1225	
28	2438.02	0.11	29	2374.72	0.112	30	2312.84	0.1262	
31	2251.13	0.1116	32	2186.42	0.1056	33	2124.82	0.0992	
34	2062.04	0.0984	35	1998.14	0.1062	36	1942.95	0.294	
37	1870.53	0.2462	38	1803.34	0.2487	39	1746.02	0.2095	
40	1678.72	0.1533	41	1601.53	1.3535	42	1583.28	0.495	
43	1543.93	0.1795	44	1494.37	3.6161	45	1493.53	4.9364	
46	1492.57	4.8165	47	1453.19	8	48	1452.31	8.4349	
49	1451.4	3.3878	50	1372.47	0.4783	51	1328.7	0.3667	
52	1311.96	0.3575	53	1241.13	0.1922	54	1181.47	0.4108	
55	1154.74	0.3807	56	1069.37	0.476	57	1028.38	0.8915	
58	1003.25	0.3071	59	980.36	0.2899	60	964.64	0.2941	
61	942.49	0.2334	62	906.75	0.5621	63	842	0.2417	
64	760.88	2.5946	65	757.22	2.8492	66	756.12	2.8298	
67	754.04	2.8285	68	752.19	2.5399	69	748.99	2.3247	
70	703.19	8	71	700.62	8	72	696.56	8	
73	620.78	0.2081	74	538.97	1.2354	75	466.16	0.1387