PerkinElmer Spectrum Version 10.4.3
Thursday, April 30, 2015 10:45 AM

Report Details
Report Location	C:\Users\Didattica\Desktop\chim_fis_2\2015\c1c2\polystirene.rtf	
Report Creator	user	
Report Date	Thursday, April 30, 2015 10:45 AM	

Spectrum
	
Name	Description	
 ___  poly	Sample 021 By ir Date Thursday, April 30 2015	

Summary
Sample Name	Description	Quality	
poly	Sample 021 By ir Date Thursday, April 30 2015	The Quality Checks give rise to multiple warnings for the sample.	

Peak Table Spectrum

Peak Table
Peak No.	X (cm-1)	Y (A)	Peak No.	X (cm-1)	Y (A)	Peak No.	X (cm-1)	Y (A)	
1	7471.8	0.0649	2	7404.77	0.0595	3	7378.08	0.0509	
4	7342.43	0.0663	5	7295.61	0.0589	6	7260.35	0.053	
7	7219.57	0.0645	8	7155.91	0.0588	9	7093.81	0.0648	
10	7038.58	0.0602	11	6969.93	0.0654	12	6909.15	0.0609	
13	6842.07	0.0657	14	6786.8	0.0609	15	6720.28	0.0656	
16	6659.43	0.0612	17	6594.05	0.0659	18	6532.29	0.0613	
19	6469.46	0.0665	20	6406.67	0.0624	21	6344.19	0.0673	
22	6280.01	0.0636	23	6215.31	0.0686	24	6156.26	0.0714	
25	6091.66	0.0739	26	6028.39	0.0752	27	5966.76	0.0944	
28	5904.46	0.0889	29	5842.26	0.0784	30	5777.74	0.0766	
31	5714.41	0.0756	32	5652.55	0.0754	33	5587.73	0.0724	
34	5526.98	0.0743	35	5463.87	0.072	36	5402.12	0.0738	
37	5338.56	0.0726	38	5276.25	0.0737	39	5213.1	0.0732	
40	5149.71	0.0738	41	5087	0.0732	42	5023.81	0.0741	
43	4960.78	0.0739	44	4899.41	0.0746	45	4834.67	0.075	
46	4772.22	0.0762	47	4709.82	0.0801	48	4654.71	0.0981	
49	4576.04	0.093	50	4521.57	0.0832	51	4457.78	0.0807	
52	4395.18	0.0852	53	4332.58	0.1004	54	4266.94	0.1054	
55	4207.06	0.1103	56	4143.68	0.0998	57	4060.88	0.1428	
58	4036.49	0.1551	59	3953.99	0.1006	60	3891.74	0.0991	
61	3827.22	0.1008	62	3766.25	0.0989	63	3701.94	0.1027	
64	3645.39	0.1135	65	3578.18	0.097	66	3514.39	0.0964	
67	3451.54	0.1005	68	3389.87	0.0968	69	3326.83	0.0967	
70	3265.45	0.0992	71	3203.17	0.1083	72	3145.37	0.1224	
73	3103.19	0.3923	74	3082.68	1.076	75	3060.45	1.4965	
76	3025.63	2.8414	77	3001.68	0.6445	78	2930.71	2.7841	
79	2927.63	2.9349	80	2925.43	3.0375	81	2923.71	3.0144	
82	2921.32	2.9608	83	2850.12	1.0282	84	2806.04	0.1619	
85	2744.35	0.1255	86	2684.36	0.132	87	2629.55	0.1329	
88	2559.87	0.1237	89	2498.16	0.1227	90	2435.76	0.1107	
91	2372.78	0.1141	92	2336.98	0.0875	93	2311.35	0.1279	
94	2248.54	0.111	95	2184.73	0.1061	96	2121.88	0.0998	
97	2059.54	0.0988	98	1991.45	0.1089	99	1943.04	0.2899	
100	1870.58	0.2462	101	1803.47	0.2504	102	1745.87	0.2093	
103	1678.19	0.1561	104	1601.56	1.3622	105	1583.31	0.4946	
106	1543.31	0.1826	107	1494.41	3.4752	108	1493.5	8	
109	1492.62	4.3047	110	1453.19	8	111	1452.31	8	
112	1372.53	0.475	113	1328.88	0.3647	114	1311.78	0.3533	
115	1240.11	0.1891	116	1181.52	0.4084	117	1154.78	0.3824	
118	1112.34	0.1893	119	1069.4	0.4735	120	1028.41	0.8911	
121	1003.28	0.3028	122	980.56	0.2892	123	964.8	0.2946	
124	942.4	0.229	125	906.66	0.5634	126	842.16	0.2421	
127	761.03	2.4882	128	758.73	3.0807	129	757.01	3.33	
130	755.36	2.9109	131	753.25	2.6104	132	751.95	2.4966	
133	749.99	2.2904	134	748.98	2.2486	135	704.44	8	
136	701.94	8	137	700.25	8	138	697.81	8	
139	696.19	8	140	694.44	8	141	620.66	0.2073	
142	540.05	1.242